## Slide 1: Developing Python code to determine the structural changes of the silica network structure in reinforced rubber
Xiaoran Wang

## Slide 2
A critical issue in the tire industry is the hysteresis loss of rubber, often attributed to the Payne effect
Payne Effect: Modulus Nonlinearity Under Strain:
1. Why is the Payne effect critical for tires?
When strain increases:
    Loss of elastic modulus
    Loss of rolling resistance
Why does the Payne effect matter?
Understanding Material Behavior
Improving tires Performance
  Material Selection and Compound Formulation
  Durability and Longevity
  Cost-Efficiency
Innovation in Tire Technologies
2. The Payne effect is attributed to:
Irreversible filler-filler network breakage
Fu & Wang, Applied Polymer Science, 2016
In the tire industry, one BIG concerns is the hysteresis loss of rubber which is believed due to the Payne effect.
Why the Payne effect matters for tire:
When the strain increases:
Loss of rolling resistance
Loss of elastic modulus
Payne Effect
filler vol%
Notes: Payne effect is a type of strain softening phenomenon observed in filled rubber: followed after a small linear elastic regime, then the pe results in a rapid decrease in storage modulus with increasing strain
There is limited evidence to confirm this due to the lack of advanced techniques for observing structural changes in nanoscale

## Slide 3
Model system
  Polymer : Polybutadiene (PB, Mw = 350 kg/mol, Mw/Mn=2.3, Asahi Kasei), Cross-linked
  Fillers: Silica (SiO2, filler size: 170 Å)
  Silane coupling agent: Bis(triethoxysilylpropyl)polysulfide (SI69, Evonik)
Sample name | “Network”
Filler volume fraction (%) | 20
Payne effect | Strain > 1%
Percolation | Yes
Network
Percolated structure
You used this figure in the previous page. Do you need again?
In general, for rheology, G’ and E’ represent the measurement mode.
G’ dynamic oscillation
E’  stretching (usually use as E Young’s modulus)
I prefer to use G’ if this comes from dynamic oscillatory mode.
To understand the mechanism underlying the Payne effect, we performed in operando X-ray Photon Correlation Spectroscopy (XPCS) experiments under oscillatory deformation for rubber samples
Aim
Notes: silica (SiO2)-filled Cross-linked polybutadiene as a rational model to study PE.
In particular, we studied the sample with 30% filler vol fraction.
We observed a significant PE when strain is greater than 1%
This sample is named as “network” based on its characteristic percolated structure formed

## Slide 4
In operando X-ray Photon Correlation Spectroscopy (XPCS)
Static structural information
(SAXS)
“Degree of correlation”
over time (XPCS)
Mimic driving
conditions
Continuous oscillatory
test for 1 h
Strain applied
Strain removed
Structural correlation
XPCS founding: Network structure is irreversibly rearranged during successive deformation under Payne effect
Notes: To mimic the real driving conditions.
Rubber samples were set for a series of cyclic tensile strains for 1hr under room temperature, meanwhile, a hard and coherent x-ray beam transmitted through the rubber samples, scattered to form speckle patterns
we got the spaced-averaged structural information on silica for each cycle from SAXS. The XPCS allows us to observe temporal fluctuations in the scattering intensity of coherent X-rays to see the correlations over time

## Slide 5
Unified (UF) equation
Koga et al, Macromolecules, 2008
Structural analysis using Small-Angle X-ray Scattering
Radius of gyration lowest lengths of aggregates the mass fractal structure
: adius of gyration
Or use this
Primary particle
Aggregate
(Rss = ?)
Aggregate
Non-Mass Fractal Agglomerate (Dm > 3)
Primary particle
(Rs=85Å)
Mass-Fractal Agglomerate (Dm = 1-3)
Notes: We used the UF equation as a mathematical model to interpret SAXS profiles
The Unified equation is particularly well-suited for studying hierarchical structures due to its ability to capture information across different length scales.

## Slide 6
strain applied
strain removed
Irreversible deformation
Before
After
F
F
F
F
Changes in SAXS profiles in term of and

## Slide 7
Challenges
    Complex fitting model
      10 variables
      Need good constraints/initial guess
    Time consuming
      Fitting ~170 SAXS curve for each experiment
      Plotting
Unified (UF) equation

## Slide 8
Approaches
Develop Python Code to:
    Extract reduced SAXS data
    Generate an initial guess based on a “good statistic” static profile
    Fit and plot SAXS profiles for each un-strained cycle
    Identify and remove outliers
    Show changes in terms of and

## Slide 9
Data extraction

## Slide 10
Define UF equation
Set upper/lower bounds
Fractal dimension: 0-5
Silica filler size: 50-85 Å
Surface fractal dimension: ~4 (smooth)
Contribution from particles are small

## Slide 11
Obtain initial guess
Differential Evolution from scipy.optimize
Differential Evolution: optimization algorithm
Randomly generate candidate solutions
Mutate 1 variable at a single time
Evaluated by cost function: Chi-square test
Replace with mutant vector
Obtain the final solution
Curve fit from scipy.optimize
Notes: It is used to find the global minimum of a multivariable function, which can be non-linear and non-differentiable. DE is particularly well-suited for optimization problems that involve a large number of variables and complex landscapes

## Slide 12
Static sample Results
Aggregate
(Rss = 333Å)
Primary particle
(Rs=85Å)
Mass-Fractal Agglomerate (Dm = 2.9)
Plot by matplotlib

## Slide 13
Oscillated Sample Results under Payne effect
0th Cycle
67th Cycle
119th Cycle
171st Cycle
Unstrained sample/ Parallel to the 10% strain direction

## Slide 14
Identify and remove outliers
linear regression
residue and standard deviation
remove outliers and refit

## Slide 15
: Radius of gyration
Not adding this?
SAXS results for Network sample at 10% strain
Cluster
Payne effect
>10% strain
NO significant strain-induced structural change was observed even at 10% strain over cycles in parallel direction.
Dm
Cycles
Dm=2
Rss=2
Rss
Cycles
Parallel direction
Payne effect has occurred at strain >1%
Notes: When we looked at our SAXS results for network sample under 10% strain where the payne effect already occurs,
Over 170 cycles, no significant structural change was obeserved in term of Dm and Rss

## Slide 16
Conclusions
Small-Angle X-ray Scattering (SAXS) is a powerful tool for investigating the intrinsic structural properties of hierarchical materials.
However, its inherent time- and space-averaging characteristics may limit its effectiveness in observing local changes
  Although the average structure of agglomerates (Network) remains unchanged, local structural variations still occur during oscillation. (from XPCS studies)
  These local changes could potentially explain the Payne effect.

## Slide 17
References
Fu, W., & Wang, L. (2016). Research on Payne effect of natural rubber reinforced by graft‐modified silica. Journal of Applied Polymer Science, 133(36). https://doi.org/10.1002/app.43891
Koga, T., Tanaka, F., Motokawa, R., Koizumi, S., & Winnik, F. M. (2008). Theoretical modeling of associated structures in aqueous solutions of hydrophobically modified Telechelic PNIPAM based on a neutron scattering study. Macromolecules, 41(23), 9413–9422. https://doi.org/10.1021/ma800957z
Rogers, M. C., Chen, K., Andrzejewski, L., Narayanan, S., Ramakrishnan, S., Leheny, R. L., & Harden, J. L. (2014). Echoes in X-ray speckles track nanometer-scale plastic events in colloidal gels under shear. Physical Review E, 90(6). https://doi.org/10.1103/physreve.90.062310